Harmonic Balance Finite Element Analysis of Third Order

Intermodulation Products in Ferrite Devices

L. Ntibarikure, G. Pelosi, S. Selleri

Department of Electronics and Telecommunications, University of Florence

Via di Santa Marta 3, 50139, Florence, Italy

stefano.selleri@unifi.it

Abstract

Results of a study of nonlinearities and intermodulation products for 3-port H-plane waveguide circulators are presented, based on a harmonic balance finite element analysis of the third-order nonlinearity in ferrites. Numerical results are derived for the field strength and the power level of the intermodulation signal.

Index Terms  Finite elements, harmonic analysis, ferrite, intermodulation, junction circulator, nonlinear interaction.

- Introduction

Waveguide devices are widely used in high-power applications thanks to their low-losses. In high-power applications for waveguide devices with ferrite inserts, the motion of the magnetization vector can no longer be described by a linear set of equations. Considering higher-order terms of the permeability, echo signals in the time domain and intermodulation coupling in the frequency domain must be included in the nonlinear theory. In particular t5hird-order nonlinearity in ferrites generate intermodulation noise in the signal bandwidth.

In a frequency domain analysis, conventional single-harmonic (SH) finite elements, does not allow for the computation of signal coupling between an in-band signal and a strong out-of-band interferer. A multiple-harmonics (MH) analysis would be an attractive alternative to time domain analysis.

The theory of harmonic balance finite element (HBFE) method, also known as multiharmonic finite element, is presented for the analysis of a generic H-plane microwave ferrite device. This technique has been successfully employed in magnetostatics problems [2]-[3] but not to high frequency ones. The final goal is to analyze a ferrite device affected by nonlinear behavior.

- Formulation

Consider a waveguide circulator (Fig. 1). Due to the H-plane symmetry of the actual 3D device, a complete solution is attained by solving the associated 2D problem just for the out-of-plane component of the electric field (Ez )

within the domain Ω, subdomain Ω1 is fully linear while subdomain Ω2 contains the nonlinear ferrite. Perfect electric conductor boundary conditions holds on Γ0 while modal expansions are enforced at ports Γi , i=1…3.  is the free space wavenumber,  is the isotropic permittivity and  has the form

where  is the angular frequency,  the gyromagnetic ratio,  the internal DC magnetic field and  the saturation magnetization. The conventional finite element formulation for anisotropic media can be retrieved in [4].

The diagonal permeability tensor coefficients can be expressed as

where Ez(r) is the electric field in the generic point r and  is a quadratic scalar operator describing the nonlinear behavior.

Considering a two-tones problem, the MH behavior is introduced by approximating the electric field as

where ω1 is the in-band signal angular frequency and ω2 is the angular frequency of the edge-band interferer, and the hat, here and in the following, denotes approximation deriving from the truncation of the series.

The complex harmonic amplitudes constitute the unknowns of a conventional finite element system, with k in (1) computed with the corresponding harmonic frequency

being c0 the speed of light in free space.

The harmonics retained in (4) are selected according to the quadratic operator , which generates third order intermodulation products, the most critical being (2ω1 - ω2) and (2ω2 - ω1). Eight harmonic amplitudes in (4) will be considered.

The nonlinear behavior of the relative permeability tensor coefficients generates coupling between the previous harmonic signals at the frequencies that expand the electric field. The dependence can be explicitated on the magnetic field as:

which constitutes a wider sum of harmonics than that of the field,  being a constant. Quadratic permeability tensor coefficients leads to the following expression

The harmonic amplitude μr of the permittivity is computed by testing its time evolving value (7) at the sought frequency

being GCD the greater common divisor function.

Harmonic testing is then performed, leading to a large scale linear HBFE system which has formally the same structure as a conventional FE system, the nonlinearity being tackled via a Picard iteration.

- Numerical results

The device analyzed is sketched in fig. 1, the ferrite parameters are those presented in [5]. For a linear ferrite the devices operates correctly as shown in Fig. 2: Devices is matched at 10GHz and isolation (S31) is better than -15dB. In the case of a nonlinear ferrite, with , analysis is performed with an impinging signal at  with an impinging power of (a) 0.5W; (b) 0.75W; (c) 1W; and an interferent signal at  with a corresponding power level of (a) 50W; (b) 75W; (c) 100W. Graph clearly shows the effect of the nonlinearity both in a frequency shift and in the presence of an output power level at the third intermodulation product.

- Conclusion

A HBFE approach for waveguide devices containing nonlinear ferrites has been presented. The proposed method allows for the prediction, in frequency domain, of the amplitude of the intermodulation products and relative signal degradation.

| Fig. 1 Sketch of the analyzed circulator H-plane cross-section. A cylindrical ferrite post of radius r is placed in the middle of the device. | Fig. 2 Amplitude of the three main scattering parameters for the linear case, for an impinging TE10. |
| --- | --- |

| Fig. 3 Amplitude of the output power at nonlinear case. (a) bullets (b) empty circles (c) asterisks. | Fig. 4 Amplitude of the output power at port 2 for the third harmonic for the nonlinear case. (a) bullets (b) empty circles (c) asterisks. |
| --- | --- |

References

[1]	B. Razavi, RF Microelectronics, Upper Saddle River NJ: Prentice Hall, 1998, ch. 2, pp.14–25.

[2]	H. De Gersem, H. Vande Sande, and K. Hameyer, “Strong coupled multi-harmonic finite element simulation package,” COMPEL, vol. 20, no. 2, pp. 535–546, 2001.

[3]	S. Yamada, K. Bessho, and J. Lu, “Harmonic balance finite element method applied to nonlinear AC magnetic analysis,” IEEE Trans. Magn.,vol. 25, no. 4, pp. 2971–2973, Jul. 1989.

[4]	M. Koshiba, and M. Suzuki, “Finite-Element Analysis of H-plane Waveguide Junction with Arbitrarily Shaped Ferrite Post,” IEEE Trans. Microw. Theory Tech., vol.34, no. 1, Jan. 1986.

[5]	N. Okamoto, “Computer-Aided Design of H-plane Waveguide Junctions with Full-Height Ferrites of Arbitrary Shape,”